## Slide 1: Technology Trends and Manufacturing Considerations for Leading Edge 3D Packaging Lithography
Robert Hsieh/Slide 1
Oct 16, 2014
Robert Hsieh, Warren Flack, Manish Ranjan
Ultratech, Inc

## Slide 2: Outline
Introduction
Reconstituted wafers
  Overlay, field size, and mapping
  Substrate handing
Interposer enabling technologies
  Lithography for Through Silicon Via
  Large Area Interposers
  Microbump Process
Conclusions
Robert Hsieh/Slide 2

## Slide 3: Introduction
To meet increasing levels of functionality and integration advanced packaging will need to support increased interconnect count and density
  Smaller CD
  Larger device area
  3D structures
Approaches for incorporation of advanced structures
  Reconstituted wafer (Fan-Out)
  Silicon interposers with through silicon via technology
Robert Hsieh/Slide 3

## Slide 4
Notes
Market Growth Potential
Timing
FUTURE
HIGH
LOW
Low cost silicon interposer solutions along with open collaboration models are expected to drive future market demand
Timing of adoption depends on thermal management, supply chain and yield solutions
Estimated wafers volume for 2017
Fan Out WLP
Si Interposer
Demand driven by server applications and potential adoption for mobile market segment
Memory Module
Mixed Device
Integration
Segment Growth Drivers
(3D Packaging)
NOW
Source: Tech Search, Internal Estimates
1.3M WPY
900K WPY
350K WPY
Robert Hsieh/Slide 4

## Slide 5
Reconstituted Wafer
Highlights
Die placement is non-systematic and printed field will have different registration errors
Critical concern is overlay to support tight design rule
Alignment mode and lithography field size considerations
Reconstituted Wafer
(Fan-Out)
Robert Hsieh/Slide 5

## Slide 6: Reconstituted Wafer Overlay
EGA overlay is not strongly affected by field size
Site-by-Site (SXS) overlay improves with smaller field size selection
5x3 Array
2x2 Array
1x1 Array
Overlay error depends on alignment method and size of exposed field
device die
Exposure field size
Robert Hsieh/Slide 6
Results from “Lithography Challenges and Considerations for Emerging Fan-Out Wafer Level Packaging Applications”, IWLPC Paper

## Slide 7: Reconstituted Wafer Overlay
Multiple Zone EGA
Separate zone EGA. Useful for separate pick and place gantry heads that creates an array shift from one tool to the other.
Useful for non-linear die drift caused by thermal processes
US Patent: 8299446
ZONE 1
ZONE 2
Overlay can be enhanced by dividing wafers in to alignment zones
Robert Hsieh/Slide 7

## Slide 8
Multiple Zone EGA Overlay
Dual zone mapping giving a tighter, more Gaussian shape to the residual error distribution
3sigma = 26.3 m
3sigma = 23.8 m
3sigma = 13.6 m
3sigma = 17.7 m
Results from “Lithography Technique to Reduce the Alignment Errors ”, IWLPC Paper
Robert Hsieh/Slide 8

## Slide 9: Warped Wafer Handling
Composite construction of reconstituted wafers results in more wafer warpage and less stiffness (sag)
Wafer automation must be capable of handling warped substrates reliably and accurately
End effector with suction cups
Chuck with enhanced flow and multiple vacuum zones
Increased height of lift pins to provide sufficient wafer clearance for robotic handling
Robert Hsieh/Slide 9

## Slide 10: Focus control on non-flat substrates
For non-flat wafer surface special focus modes can be used to enhance focus control
Grid Focus Mode
Generates focus map of entire wafer before exposure
Determines local tilt and applies corrections during exposure
Red dots are field corner borders where focus is measured
At wafer edge additional focus measurements are made
Robert Hsieh/Slide 10

## Slide 11: Silicon Interposer
Highlights
Si interposer technology is expected to gain significant traction for leading edge devices
Improved device performance of FPGA and GPU devices is expected to drive requirements
Si Interposer Structure
Robert Hsieh/Slide 11

## Slide 12: Si Interposer Enabling Technologies
Implementing silicon interposer requires development of new process technologies
  Embedded target alignment for Through Silicon Via
    IR Alignment system
    Metrology
  Large area devices
    Field stitching
  Microbump
    Attach dies to the interposer
Robert Hsieh/Slide 12

## Slide 13: Embedded target alignment
For Via Last process to form Through Silicon Vias the device layers and alignment targets are viewed through silicon
Process requires thinning the silicon with uniform thickness and polished surface for best image contrast
Robert Hsieh/Slide 13

## Slide 14: Stepper Self Metrology for Dual Side Alignment
Front side metrology
silicon
carrier
camera
photoresist
Z offset
Alignment system
Back side metrology
silicon
carrier
camera
photoresist
IR transmits through silicon
Top directed illumination allows for flexible placement of targets on the wafer
Off axis IR camera implemented on stepper
Measure XY positions of two features at different Z heights
200 micron thick silicon
Results from “Verification of Back-To-Front Side Alignment for Advanced Packaging”, IWLPC Paper
Robert Hsieh/Slide 14

## Slide 15: DSA Stepper Self Metrology
Embedded test wafers prepared using a copper damascene process
Wafers were thinned to thicknesses of 100, 200 and 300 microns and bonded to a carrier
Wafers were exposed on an AP300 stepper with DSA
Stepper self metrology was performed to collect data on five sites per field in eleven fields for a total of 55 sites per wafer
Mean plus three sigma was less than 1.0 micron for all three thicknesses of Si
Results from “Verification of Back-To-Front Side Alignment for Advanced Packaging”, IWLPC Paper
Robert Hsieh/Slide 15

## Slide 16: Large Area Interposer Lithography
Since large area interposer may be larger than the stepper field, the pattern can be constructed from multiple sub-fields
Test interposer design consists of a top half and bottom half
For stepper patterning both top and bottom sub-fields can fit onto a single 1X reticle
Wafer layout with stitched interposer
Standard configuration with two stepper fields can support up to 52 x 52 mm maximum square interposer
Robert Hsieh/Slide 16

## Slide 17: Stitching Performance Test Structures
Serpentine/Comb structure to test integrity of lines crossing the stitch
varying line/space pitch arranged from left to right, with smallest CD of 1.5 µm Line/Space
Line and Space structure with varying line/space pitch arranged from left to right, with smallest CD of 1.5 µm Line/Space
Stitch boundary contains multiple sets having different Y overlaps. For this set the top label denotes a 0.5 µm overlap.
Variable X offsets can be intentionally introduced between the top and bottom half
Top half exposure
Bottom half exposure
stitch line denotes sub-field boundary
Results from “Large Area Interposer Lithography”, ECTC Paper
Robert Hsieh/Slide 17

## Slide 18: Electroplated Cu Across the Stitch
Top down view of Cu plated metal lines (a) before Cu seed etch and (b) after seed etch, for 3 µm pitch, line and space pattern
Line edge roughness becomes significant percentage of linewidth for smaller CDs
Line edge roughness can be reduced by using very thin seed layer
Results from “Large Area Interposer Lithography”, ECTC Paper
Top half exposure
Bottom half exposure
Stitch line
Robert Hsieh/Slide 18

## Slide 19: Intentional Offset Stitching Tests
3 µm pitch line/space structure
3.5 μm thick positive photoresist
Y overlap varied between ±1 μm
X stitch offset set at +0.25 µm
Resist
Top half exposure
Bottom half exposure
Results from “Large Area Interposer Lithography”, ECTC Paper
Stitch line
Robert Hsieh/Slide 19

## Slide 20: Electroplated Cu Structures Across Stitch
Cu electroplated serpentine/comb structure with a 3 µm pitch with no offsets. Visual inspection reveals no line breaks or shorts in the structure.
SEM of electroplated metal lines with introduced lateral offset at the field stitch of 0.25 µm.
Pitch = 6 µm
4 µm line, 2 µm space
Pitch = 4 µm
Pitch = 3 µm
Results from “Large Area Interposer Lithography”, ECTC Paper
Robert Hsieh/Slide 20

## Slide 21: Modeling of Field Stitching
Simulated conditions for stitching line with square ends and 45 degree tapered ends
Varied lateral offset and vertical overlap
Top and bottom exposures are independently simulated
Top half exposure
Bottom half exposure
Top half exposure
Bottom half exposure
Results from “Large Area Interposer Lithography”, ECTC Paper
Square Line Ends
Tapered Line Ends
Robert Hsieh/Slide 21

## Slide 22: Simulated Stitch Performance for Square and Tapered Line Ends
+10%
-10%
nominal CD
Data from Prolith modeling of JSR IX845 resist for nominal linewidth of 1.5 µm.
The overlap range is 25% larger for the tapered line end relative to the square line end for a ±10% CD tolerance
Results from “Large Area Interposer Lithography”, ECTC Paper
Robert Hsieh/Slide 22

## Slide 23: Microbump Lithography
Application includes 3D die-to-die and die-to-wafer stacking and interposers.
Maintaining lithographic process control for microbumping is challenging due to the small bump diameters and high aspect ratios.
Microbumps are formed by electroplating Cu inside 3.5 µm vias printed in 13.2 µm thick photoresist
3.5 micron microbump
Robert Hsieh/Slide 23

## Slide 24: Microbump Experimental Results
3.5 µm CD with 10.0 mm pitch, AZ EM 10XT resist thickness is 13.2 mm
Process requirements are bottom CD of 3.5 µm ± 10% and sidewall angle > 87 degrees
CD data collected by top-down SEM and sidewall angle collected by cross-sectional SEM
Process Window DOF is 10.0 mm
Cross Section at Focus = 0 mm
Results from “Microbump Lithography for 3D Stacking Applications”, IWLPC Paper
Robert Hsieh/Slide 24

## Slide 25: Microbump Lithography Simulation
Process Window
Cross Section at Focus = 0 mm
Simulations using KLA-Tencor Prolith (version14.1.1.1)
3.5 mm CD with 10.0 mm pitch, resist thickness is 13.2 mm
Process requirements are bottom CD of 3.5 mm ± 10% and sidewall angle > 87 degrees
Results from “Microbump Lithography for 3D Stacking Applications”, IWLPC Paper
Robert Hsieh/Slide 25

## Slide 26: Microbump Process Scalability
2.5 mm CD
DOF is 9.9 mm
2.4 mm CD with 0.1 mm bias
DOF =12.3 mm
Photoresist simulation can be used to predict lithographic performance
2.5 mm CD with 7.0 mm pitch, resist thickness is 10.0 mm
Process requirements are bottom CD of 3.5 mm ± 10% and sidewall angle > 87 degrees
Results from “Microbump Lithography for 3D Stacking Applications”, IWLPC Paper
Robert Hsieh/Slide 26

## Slide 27: Conclusions
Lithography capability is critical for extending advanced packaging technologies
Reconstituted Wafers
  Importance of EGA versus Site-by-Site alignment for throughput
  Multiple zone EGA developed for improved overlay while maintaining high throughput
  Warped wafer handling and focusing modes for non-flat wafers
Silicon Interposer Technology
  Back-to-Front Side Alignment and Metrology
    Alignment to embedded targets can be monitored using stepper self metrology
  Large Area Interposers
    Experimentally investigated patterning copper lines with lateral dimensions as small as 1.5 µm line/space in a vertically stitched large area interposer
  Microbump Lithography
    Experimentally investigated 3.5 mm microbumps with a 10.0 mm pitch
    Used resist modeling to predict the performance of 2.5 mm microbumps and ways to optimize the process window
Robert Hsieh/Slide 27